APPLICATION OF NATURAL DYES ON COTTON PINEAPPLE BLENDED FABRIC BY VARYING MORDANTS

C.Saranya

Assistant Professor

Department of Costume Design and Fashion, Kongu Arts and Science College (Autonomous), Erode, India

Email: csaranyacdf@gmail.com

_____________________________________________________________________________________________________________________

ABSTRACT

Natural dyes find use in the colouration of textiles, foods, drugs, and cosmetics. Recently, the use of natural dyes in textile industry has gained more significant attention owing to environmental concern on the use of certain toxic synthetic dyes. The importance of natural dyes is realized worldwide because of its eco friendliness. Various attempts have been made globally to extract natural dyes from different natural resources and to apply on textile materials. In this research, Cotton and Pineapple blended fabrics are dyed with natural dyes extracted from Marigold flower. In this study, Myrobolan,Ferrous Sulphate ,Aluminum potassium sulphate (Alumn),Potassium dichromate ,Copper Sulphate are used as a mordant for dyeing Cotton and Pineapple fibre blended fabric. Reaction of the marigold dye with different mordants will create different colour shades. Anti-microbial properties for the Marigold dyes are reported. The result on colour fastness to washing and light, as well as fabric weight, fabric thickness, drapability, fabric stiffness, tensile strength of the dyed fabrics are also reported.

Keywords: Marigold dye, Cotton and pineapple fibre, Myrobolan, Antimicrobial properties

INTRODUCTION

Textiles have such an important bearing on our daily lives that everyone need to know something above them from earliest times  .Pineapple fiber yarn is extracted from the pineapple plant. Extraction of fibers means separation of fibers from the commenting subtonics such as pectin’s or lignin’s wax resins, fats and other carbohydrates, fibers from vegetable plants are extracted by mechanical retting.The leaves of pineapple plant contain approximately 3% of strong white silky fibers .The extracted fiber is knotted by hands and made into yarn. Pineapple fiber yarn gives luster as like silk. It is little course fiber then silk. Cotton is an element which transforms the entire life of fabric. Cotton is a soft fluffy stable fiber . The fiber is almost pure cellulose the botanical purpose of cotton fiber is to aid in seed dispersal.

Natural dyes are safer, easy disposal, eco friendliness and some dyes have medicinal properties that will improve value addition to the product. Marigold plant is a stout branching herb, very popular as a garden as a garden plant for us bright coloured flowers. The flowers are lemon yellow or orange in colour. The flower heads yield a shinning yellow dye flowers bloom abundantly from the beginning of summer upto autumn and even faded flowers are rich in dyeing pigment. Marigold dye can range is colour from a brilliant, sunny yellow to a deep crimson, depending on the colour of the flower. Marigold has anti-septic, and anti-fungal properties.In this study, cotton and pineapple blended yarn is converted into plain woven eco-friendly fabric dyed with natural dyes.

OBJECTIVES OF THE STUDY

- To extract the pineapple fiber from the leaf of the pineapple plant.

- To blend cotton and pineapple fiber into 40s count yarn.

- To weave the pineapple fiber and cotton blended yarn with plain weave.

- To treat the fabric with different mordants.

- To dye the above fabric using natural Marigold flower dye.

- To test the dyed fabrics for the required qualities .

MATERIALS AND METHODS

SELECTION OF YARN

75% pineapple fibre  + 25% cotton blended yarn

SELECTION OF COUNT

40 s count

SELECTION OF WEAVE

Plain weave

PREPARATION OF FABRIC FOR DYEING

SCOURING

Pineapple and cotton blended fabric is washed in a solution containing 0.5gk sodium carbonate and 2gk nonionic detergent solution at 50oC for 25 min keeping the material is to liquor ratio at 1:40. The scoured material is thoroughly washed with water and dried at room temperature. The scoured materials are soaked in clean water for 30 min prior to dyeing or mordanting

SELECTION OF MORDANT

- Myrobolan

- Ferrous Sulphate

- Aluminum potassium sulphate (Alum)

- Potassium dichromate

- Copper Sulphate

MORDANTING

Accurately weighed cotton and pineapple fibre blended fabric sampleis treatedwith different mordants-Myrobolan (PC1 ), Ferrous Sulphate (PC2 ), Alum (PC3), Potassium dichromate (PC4 )& Copper Sulphate (PC5 ). The scoured fabric is then subjected to heating. Temperature of the dye bath is raised to 80oC over a period of half an hour and left for another 30 minutes. The materials are then rinsed with water thoroughly, squeezed and dried. Finally the fabrics are subjected to dyeing because mordant is very sensitive to light.

SELECTION OF DYE

Marigold Dye

PREPARATION OF MARIGOLD DYE EXTRACT

The fresh petals of Marigold are shadow dried and made into a fine powder. Dry powder is then mixed with 99.9% absolute ethanol in the ratio of 1:5 in a beaker. The beaker is placed in the shaker and allowed overnight to 40oC so that the ethanol takes in the active components of the petals. Then the solution is centrifuged and filtered using filter paper. The clear solution is powder onto the petri plates and placed in the hot air oven set at 80oC and ethanol is allowed to evaporate for 1 hour. Now the marigold due is extracted and ready to use it for dyeing.

METHOD OF APPLICATION

Dip dyeing method

NOMENCLATURE OF THE SAMPLES

| S.No | SAMPLE CODE | YARN USED | WEAVE | MORDANT USED | DYE USED |
| --- | --- | --- | --- | --- | --- |
| 1 | PC1 | 75% pineapple + 25% cotton blended yarn | Plain weave | Myrobolan | Marigold Dye |
| 2 | PC2 |  |  | Ferrous Sulphate |  |
| 3 | PC3 |  |  | Aluminum potassium sulphate (Alum) |  |
| 4 | PC4 |  |  | Potassium dichromate |  |
| 5 | PC5 |  |  | Copper Sulphate |  |

RESULTS& DISCUSSION

Physical tests

Fabric Weight

It is evident that there is a slight difference in fabric weight of the dyed samplescompared to  original sample. Sample (PC2) showed maximum weight compared to other samples.

Fabric Thickness

It is found that the fabric thickness of the sample (PC3) has slight increase compare to the others.

Tensile strength

It is evident that the tensile strength is more in sample (PC2) and sample (PC4) in warp and weft direction respectively.

Stiffness test

It is found that bending length in the warp way  direction is high in sample (PC5) , in weft way direction the bending length is high in sample  (PC3).

Fabric Drape

It is revealed  that the drapability of pineapple cotton fabric  dyed with marigold dye is good .

Colour fastness test

- Colour Fastness to Light&washing

Colour fastness to light and washing is very good in Sample PC4

Antimicrobial test:

Mycelia growth test

It is found that there is a reduction in the growth of mycelia (fungus) in all the treated samples when compared to untreated fabric samples. The 100% treated sample shows maximum anti microbial activity than others.

FABRIC WEIGHT

Table – I

| S. No | Sample | PC in GSM |
| --- | --- | --- |
| 1 | PC1 | 80 |
| 2 | PC2 | 82 |
| 3 | PC3 | 77 |
| 4 | PC4 | 70 |
| 5 | PC5 | 78 |

FIGURE – I

FABRIC THICKNESS

Table - II

| S. No | Sample | PC in mm |
| --- | --- | --- |
| 1 | PC1 | 15 |
| 2 | PC2 | 13 |
| 3 | PC3 | 16 |
| 4 | PC4 | 15 |
| 5 | PC5 | 14 |

FIGURE - II

TENSILE STRENGTH

Table III

| S. No | Sample | WARP WAY |  | WEFT WAY |  |
| --- | --- | --- | --- | --- | --- |
|  |  | Tensile Strength In 1bs | Elongation in Inch | Tensile Strength In 1bs | Elongation in Inch |
| 1 | PC1 | 70 | 2.5 | 50 | 2.1 |
| 2 | PC2 | 80 | 2.9 | 60 | 2.3 |
| 3 | PC3 | 60 | 2.7 | 55 | 2.2 |
| 4 | PC4 | 75 | 2.6 | 65 | 2.5 |
| 5 | PC5 | 50 | 2.2 | 45 | 1.8 |

FIGURE - III

TENSILE STRENGTH BREAKING LOAD

TENSILE STRENGTH ELONGATION

FABRIC STIFFNESS

Table VI

| S.No | Sample | Stiffness in warp direction | Stiffness in weft direction |
| --- | --- | --- | --- |
|  |  | Bending length in (Cms) | Bending length in (Cms) |
| 1 | PC1 | 3.2 | 2.6 |
| 2 | PC2 | 3.1 | 2.5 |
| 3 | PC3 | 3.2 | 2.7 |
| 4 | PC4 | 3.3 | 2.6 |
| 5 | PC5 | 3.4 | 2.5 |

FIGURE – IV

FABRIC DRAPE

Table V

| S.No | Sample | Drapability of PC fabric in percentage |
| --- | --- | --- |
| 1 | PC1 | 24.7 |
| 2 | PC2 | 25.3 |
| 3 | PC3 | 25.8 |
| 4 | PC4 | 24.9 |
| 5 | PC5 | 26.1 |

FIGURE – V

FABRIC DRAPE

COLOUR FASTNESS TEST

TABLE - VI

| S. No | SAMPLE | COLOUR FASTNESS TO LIGHT |  | COLOUR FASTNESS TO WASHING |  |
| --- | --- | --- | --- | --- | --- |
|  |  | After 5 Hrs | After 10 Hrs | Change in colour | Staining on sample |
| 1 | PC1 | ¾ | 3 | 3 | ¾ |
| 2 | PC2 | 4 | 4 | 4 | ¾ |
| 3 | PC3 | ¾ | 3 | 3 | ¾ |
| 4 | PC4 | 4/5 | 4 | 4 | 4/5 |
| 5 | PC5 | 3 | 3 | 3 | 3 |

- Very poor ,  2.Poor , 3. Mordent , ¾ Fair , 4. Good , 4/5 Very Good , 5. Excellent

CONCLUSION

The investigator has given a conclusion that the pineapple filament is strong when it is blended with cotton .The fabric is pre-treated with different  Mordants.then the fabric is dyed with  Marigold  dye. Reaction of Marigold dye with different mordantscan  produce different shades. Marigold dye can control the growth of microbes. The combination of pineapple cotton blended fabric with marigold dye with different mordant  has antimicrobial property and it is a ecofriendly fabric.

REFERENCES

- Textile Dyer & Printer, 1996, 29, October  Paul R. MalankerJ.V and Naik  P. 16-24

- Indian Journal of Fiber & Textile Research, 2006, 31,December 583- 587  Li.W. and X.W, P. 219

- Mahale G , Sunanda R K and Sakshi  ,C olour fastness of eco dyed cotton with Marigold ,Text trends, 2000, P. 35-39